AMERICAN COATINGS

TL-1 EPOXY

LAMINATING COATING

A 100% solids epoxy for laminating with fiberglass for a 62 mil lining system.

# GENERAL FEATURES

- EXCELLENT CHEMICAL RESISTANCE

- SPRAYABLE

- HIGH FILM BUILD

- PROCESS EQUIPMENT COATING

# DESCRIPTION

100 solids to minimize shrinkage.  A chemical resistant epoxy coating with exceptional adhesion to various substrates.  Excellent resistance to petroleum products, alkalies, salts, organic solvents and gases.

# USES

As a resin binder for reinforcing fiberglass mat or chopped fiberglass to produce a protective coating and lining, where excellent chemical resistance is required for the protection of interior tank bottoms exposed to sour crude, gasoline, military fuel, salt water and other petroleum products.  Also, for the protection of exterior tank roofs under severe chemical exposures.

PROPERTIES

Hardness (Rockwell M)-------------------------------105-120

Strength: (Lbs. X 10³) Adhesive-----------------------1.6-2.7

# (PSI X 10³)    Compressive-------------------50-90

Flexure------------------------ 45-80

Shear---------------------------17-22

Tensile-------------------------33-50

# PHYSICAL DATA

Finish ------------------------------------------------------ Gloss

Color ---------------------------------------------------- Various

Applied Over ---------------------------------------------- Steel   Components ------------------------------------------------Two

Cure ---------------------------------------------------- Catalytic Mix ratio-------------------------------------------------------2:1

Volume Solids   2% ---------------------------------- 100%

## Recommended Dry Film

Thickness ------------------------------- 62 mils w/fiberglass

Application Method -------------- Airless plural component

Thinning Required------------------------ DO NOT THIN.

CureTime @ 77F and 50%  RH:

Recoat ------------------------------------------  Within 24 hrs.

Hard Dry ------------------------------------------- 12 – 24 hrs.

Topcoat --------------------- Alkyds, Epoxies, Polyurethane

(Inorganic Zinc is not recommended)

Maximum re-coat interval at 77F or less----------30 days

Coverage With Glass:

Recommended Thickness----------------------- 25 sq. ft/gal

## Temperature Limit

Immersed ------------------------------------------------- 190F

Atmospheric --------------------------------------------- 250F

## Miscellaneous Properties

Shelf Life ------------------------------------------------- 1 Yr.

Pot Life – Mixed @ 77F ---------------------- 45 – 60 Min.

Pot life accelerates greatly at elevated temperatures.

# SURFACE PREPARATION

Near White Sandblast SSPC-SP10-63.

# TL-1

# APPLICATION INFORMATION

Do not apply if temperature is below 50F and/or above 85% relative humidity.

## APPLICATION METHOD

Airless spray plural component process equipment.

MIXING

Power agitate each component thoroughly.

# CLEAN-UP AND THINNING

Thinning is not recommended.  Clean up tools and equipment with TH 760 thinner.

SPRAY EQUIPMENT

Pump Ratio ------------------------------------------------- 30:1

Air Supply (in) ----------------------------------------- 100 psi

Hose Diameter (ID) ----------------------------------------- ¼”

Hose Length (max) ----------------------------------------- 75’

Tip Size ----------------------------------------------------- .027

Atomization Pressure (psi) ----------------------------- 2,400

SAFETY INFORMATION

WARNING!  COMBUSTIBLE, HARMFUL IF INHALED, CAUSES IRRITATION

Keep away from heat, sparks or flame.  Use with adequate ventilation.  Do not breathe vapors or spray mist.  Wear an appropriate, properly fitted respirator during and after application unless air monitoring demonstrates vapor/mist levels are below applicable limits.

SHIPPING DATA

Proper Shipping Name -------------------------- Paint Liquid

Hazard Class----------------------------- Combustible Liquid

Flash Point F SETA

Part A --------------------------------------------------- 200F

Part B --------------------------------------------------- 200F

UN No.------------------------------------------------------ 1263

### PACKAGING

PART A

Fives -------------------------------------------------- 52.50 lbs.

PART B

Fives--------------------------------------------------  45.50 lbs.

DISCLAIMER

The facts stated and the recommendations and suggestions herein are based upon experiments and supplier information believed to be reliable.  No guarantee is made of their accuracy, however, and American Coatings ASSUMES NO LIABILITY FOR  PRODUCT FAILURE OTHER THAN TO SUPPLY REPLACEMENT MATERIAL FOR PRODUCTS SHOWN TO BE DEFECTIVE WHEN DELIVERED OR TO REFUND THE  PURCHASE PRICE.  Except as stated, THERE ARE NO WARRANTIES, EITHER EXPRESSED OR IMPLIED, OF MERCHANTABILITY, FITNESS OR OTHERWISE.  AMERICAN COATINGS SHALL NOT BE LIABLE FOR SPECIAL, INCIDENTAL AND CONSEQUENTIAL DAMAGES.  No statement contained herein shall be constructed as an inducement to infringe existing patents or as an endorsement of specific manufacturers.										10/2011